## Slide 1: TexGen Workshop
Dr Louise Brown
https://github.com/louisepb/PurdueWorkshop2019

## Slide 2: Composites Research Group
University of Nottingham

## Slide 3: Composites Research Group Overview
Head of Group – Prof Xiaosu Yi
4 academics
4 Research Fellows
5 PhD students
Head of Group – Prof Nick Warrior
12 academics, including 5 professors
11 researchers
20 PhD/EngD students
Head of Group – Dr Albert Tshai
4 academics
5 PhD students
Advanced Manufacturing Building
Jubilees Campus, Nottingham
Due Dec 2017
£24m investment
9000m2 over 3 floors
600m2 composites lab space
UK Research Portfolio (£14.5m)
EPSRC Future Composites Manufacturing Hub - £10.3m *
Other EPSRC - £265k
Innovate UK - £810k
Industry - £1.5m
European Commission - £1.1m
Other - £500k
(* Includes funding for other Hub members)

## Slide 4: UoN Research Portfolio
Composites Manufacturing
Mechanical and Failure
Textile Composites
Bio-composites
Composites Recycling
EPSRC Future Composites Manufacturing Hub – Automated Dry Fibre Placement
Advanced Manufacturing Supply Chain Initiative (AMSCI) – ProPound
Composites Innovation Cluster (CiC)
Affordable Lightweighting Through Pre-Form Automation (ALPA)
Thermoplastic Overmoulding for Structural Composite Automotive Applications (TOSCAA)
Boeing – Nottingham Strategic Collaboration
Towards Affordable, Closed-Loop Recyclable Future Low Carbon Vehicle Structures (TARF-LCV)
Markets for fluidized bed carbon fibre recycling
Graphene-based Electrodes for Application in Supercapacitors (ElectroGraph)
AVIC – Nottingham University Innovation Centre
  Buckling analysis software of stiffened panel structures
  Impact damage in composite components
  Design and strength analysis of braided composites
Biaxial material testing
Tack testing of prepregs and ATL tapes
SAFE-FLY EID
Bioresorbable Engineering Nanocomposites for Healthcare (BENcH)
In situ polymerization of bioresorbable composites
Resorbable fibre textile manufacture
Production of commercially scalable multifilament phosphate fibre tows
Processing and performance of polymer matrix composites
Interests in both thermoset and thermoplastic matrices
Emerging interests in novel metal materials and hybrid structures
EPSRC Future Composites Manufacturing Hub – Textile Optimisation
EPSRC RSE Fellowship – Texgen
Damage Modelling of Composites (Variability in Textiles)
Friction in composites forming
BAM – Breakthrough Aerospace Material

## Slide 5: General Overview of the TexGen Project

## Slide 6
TexGen Geometric Textile Modelling Software
Fibre/Micro-Scale
Unit Cell/Meso-Scale
Component/Macro-Scale
Generate textile geometry using TexGen GUI or script
Automatically generate 2D and 2D sheared textiles
3D wizard generates idealised 3D textiles
Refinement of orthogonal weave to simulate compaction
Generate mesh and input files for FEA or CFD to predict material properties
Micro-scale FEA simulations or analytical methods determine yarn properties
Composite material properties extracted from meso-scale predictions are used to model structural components

## Slide 7: TexGen Webpage
www.texgen.sourceforge.net

## Slide 8: Download TexGen
https://sourceforge.net/projects/texgen/
Use the Files tab to access different versions and installation files with and without bundled Python

## Slide 9: Code on GitHub
Source code is stored on GitHub
https://github.com/louisepb/TexGen
Instructions for compiling from source for both Windows and Linux are here:
http://texgen.sourceforge.net/index.php/Compiling_from_Source
Bugs/issues can be reported here:
https://github.com/louisepb/TexGen/issues
Sample scripts are here:
https://github.com/louisepb/TexGenScripts

## Slide 10: TexGen Forum
Queries about TexGen can be directed via the TexGen forum
http://texgen.sourceforge.net/phpBB3/index.php
This is also a useful source of information and gives a record of queries and discussion by other TexGen users

## Slide 11: Implementation
Modular - Core functionality is in the core module, graphics are in a renderer module; if not using visualisation, the renderer doesn’t need to be built.
Platform independent – Can be run on most operating systems supported by the Cmake build system.
Flexible – Can be used with the GUI, using SWIG generated Python code or used as a library of C++ functions

## Slide 12: TexGen Class Hierarchy

## Slide 13: TexGen Use Cases

## Slide 14: Permeability and Mechanical Modelling

## Slide 15: Advanced Geometry Modelling of 3D Woven Reinforcements in Polymer Composites: Processing and Performance Analysis
X. Zeng, L.P. Brown, A. Endruweit, A.C. Long
X Zeng, L P Brown, A Endruweit, A C Long. “Advanced geometry modeling for 3D woven fabrics in composites processing and performance analysis”, Proc. 4th World Conf. on 3D Fabrics & their Applications, Aachen, Germany, Sept 2012.

## Slide 16
Geometrical modelling
acquisition of detailed geometry data (m-CT scanning)
generation of geometrical model in TexGen
Example:
orthogonal carbon fibre weave
Fabric style | Orthogonal weave
Areal density (kg/m2) | 4.775
Number of warp layers | 6
Warp yarn | 12K
Warp yarn linear density (g/km) | 800
Number of weft layers | 7
Weft yarn | 6K × 2
Weft yarn linear density (g/km) | 800
Binder yarn | 1K
Binder yarn linear density (g/km) | 67

## Slide 17
TexGen unit cell model
CFD simulation of steady-state Stokes flow
Fabric permeability
Determine in-plane and through-thickness permeabilities from prescribed pressure gradients and calculated average flow velocities
Impregnating resin flow in composites processing is described by homogenisation of local flow through pore spaces in the textile unit cell
generation of voxel mesh
(streamlines for flow along warp direction)
(Ansys CFX)

## Slide 18
Geometry refinement
Experimental permeability data
Simulation with straight yarns, constant elliptical cross-section
Varying binder cross-section, weft and warp yarns straight, constant cross-section
Deformation of weft yarns on fabric surface
Yarn cross-sections ‘more rectangular’ in warp direction than in weft direction
Increasingly accurate modelling of yarn geometries

## Slide 19
Compression modelling
cycle 5
cycle 1
binder “buckling”
yarn flattening, widening
Quasi-static compression (5 mm/min) between flat parallel plates,
1 fabric layer
3.94 mm
5.88 mm

## Slide 20
Vf = 0.55
Vf = 0.67
Vf = 0.55, h = 5 mm
Vf = 0.65, h = 4.2 mm
Experimental geometry analysis: top layer of weft yarns on fabric surface
Geometry modelling of fabric at different compaction levels
Compression modelling
details of complex deformation difficult to reproduce accurately !

## Slide 21
Kozeny-Carman fit
Kozeny-Carman fit
Discontinuity in K1 is related to change in binder configuration on fabric surface;
not described by analytical permeability models, requires numerical analysis
top layer of weft yarns on fabric surface
Vf = 0.55
Vf = 0.65
(permeability along weft-direction)
(permeability along warp-direction)
Compressed permeability
experiment
CFD
experiment
CFD

## Slide 22
Moulding of composite plaques by vacuum-driven RTM:
1 fabric layer
Gurit PRIME 20LV epoxy infusion system
composite was tested in warp- and weft-direction
h = 5 mm, Vf = 0.55
Tensile testing according to
European Standard EN ISO 527-4:1997
Composite mechanical properties
 | E / GPa | Tensile strength / MPa | Tensile failure strain / % | Interlaminar shear strength / MPa
Cured resin | 3.5 | 73 | 3.5 | 47
Fibre: Toray T300 | 230 | 3450 | 1.5 | -
Nominal material data for numerical analysis

## Slide 23
Finite element analysis for calculation of elastic properties for composite (impregnated yarns), assuming hexagonal packing of filaments:
six load cases of a single filament (+ resin) unit cell model
Yarn mechanical analysis
E11
E22
E33
G12
G13
G23
(ABAQUS)
alternative: micromechanics equations (Chamis)

## Slide 24
Properties of impregnated yarn, derived from FE analysis, fibre Torayca T300
Vf = 0.66 in yarn, corresponding to Vf = 0.55 in unit cell
E11 | E22, E33 | G12, G13 | G23 | ν12, ν13 | ν23 | F11 | F22 | F12
152.6 GPa | 8.15 GPa | 3.02 GPa | 2.9 GPa | 0.3 | 0.345 | 2289 MPa | 69.6 MPa | 47 MPa
Yarn mechanical analysis
ILSS
from fibre failure strain
resin tensile strength
longitudinal:
maximum stress
transverse:
maximum principal stress
shear:
partial distortion energy
Ruijter, W., Analysis of mechanical properties of woven textile composite as functions of textile geometry, PhD dissertation, University of Nottingham, 2008
Failure model (Ruijter):
longitudinal: brittle failure (fibres)
transverse, shear:
gradual stiffness reduction (matrix)
c1 = 8, c2 = 13
(empirical)

## Slide 25
Assignment of local properties + orientations to TexGen voxel mesh of composite unit cell for mechanical FE analysis
Unit cell mechanical analysis
simulation
experiments
(5 repeats)
warp-direction
experiments
(4 repeats)
simulation
 | warp |  | weft | 
 | F / MPa | E / GPa | F / MPa | E / GPa
simulation | 845 | 64 | 669 | 64
experiment | 791  38 | 60  2 | 710  21 | 58  3
voxels representing resin only are not shown
weft-direction

## Slide 26
Unit cell mechanical analysis
failure strain similar in both directions
difference in strength is related to ratio of fibre volume in both directions, if surface layers are discounted
Comparison of calculated properties in warp- and weft-direction
crimped surface layers in weft-direction contribute little to strength
predicted failure of crimped surface layers
warp
weft

## Slide 27
Unit cell mechanical analysis
Influence of voxel mesh density,
for weft yarns only
significant difference in failure strain
coarse
fine
artefacts in geometry meshing affect simulation results

## Slide 28
Conclusions
For a 3D orthogonal weave, the architecture was characterised in detail by analysis of m-CT images of composites.
Geometrical unit cell models were generated in TexGen in a semi-automated manner.
Fabric permeability predictions based on simulations of impregnating flow
improved significantly in accuracy with increasing level of detail in geometrical modelling
indicated that binder configuration on fabric surface has significant effect on weft permeability
Composite strength predictions based on static mechanical analyses
showed good quantitative agreement with experimental results
indicated reduced strength in weft-direction, mainly due to crimp in surface layers

## Slide 29
Acknowledgement
This work was supported by the Engineering and Physical Sciences Research Council [grant number: EP/IO33513/1], through the EPSRC Centre for Innovative Manufacturing in Composites.
3D woven fabric was supplied by Airbus UK.

## Slide 30: Coefficient of Thermal Expansion

## Slide 31: Predicting the Coefficient of Thermal Expansion for Textile Composites Based on a Unit Cell Approach
Louise P. Brown, Xuesen Zeng, Andrew C. Long, Richard Brooks, I. Arthur Jones
L P Brown, X Zeng, A C Long, R Brooks, I A Jones. “Predicting the coefficient of expansion for textile composites based on a unit cell approach”, Proc. 11th Int. Conf. on Textile Composites (TexComp-11), Leuven, Sept 2013.

## Slide 32
Objectives
To predict coefficients of thermal expansion (CTEs) for sheared woven fabric laminates, which have been characterised through experiments.
To improve the quality of prediction by automated creation of realistic geometries in TexGen
Sources of shear deformation
Fabric forming
Manufacturing defects caused by material handling

## Slide 33
Sheared Textile Modelling
Extension to existing 2D weave wizard
Input shear angle
Optional sheared domain
Max intersection depth = 0.034mm

## Slide 34
Sheared Yarn Rotation Angle
Calculation of rotational angle at yarn crossover to avoid intersections

## Slide 35
Intersection correction
Algorithm already implemented for non-sheared 2D weaves
Creates polygon cross-sections
Results in loss of yarn volume
Cross-section adjustment
Tow drop offset
Modifier = 1: Cross-section point is on domain plane
Modifier < 1: Intersection with plane lies inside yarn volume. Modifier applied. Iterative method used to adjust cross-section points to restore original cross-sectional area
Modifier > 1: Shown in figure. No adjustment required
Cross section adjustment

## Slide 36
Refined Sheared Textile
Unrefined, 15°
Refined, 15 °
Max intersection depth = 0.034mm
Max intersection depth = 0.0015mm

## Slide 37
CTE Prediction of Sheared Laminates
Abaqus input file is generated automatically within the TexGen GUI
Compatible voxelised mesh is created with periodic boundary conditions

## Slide 38
Shear domain periodic boundary conditions
Face C
Face D
Edge 3
Edge 4
Edge 1
Edge 2
Face E (F)
Edge 7(6)
Edge 8(5)
Edge 11(10)
Edge 12(9)
Node 5 (1)
Node 6 (2)
Node 7 (3)
Node 8 (4)
Face A
Face B
Li, S., C.V. Singh, and R. Talreja, A representative volume element based on translational symmetries for FE analysis of cracked laminates with two arrays of cracks. International Journal of Solids and Structures, 2009. 46(7–8): p. 1793-1804.
x
y
Shear angle
β
Face A & B relative displacement
Face C and D:
Faces E and F orthogonal to Z (Thickness C)
Edges:
Vertices:

## Slide 39: Thermal mechanical analysis
ABAQUS static analysis, perturbation
Temperature change 1oC
CTEs are recovered directly from unit cell strain tensor:
Chart: Mesh convergence
| 50000 | 98000 | 112500 | 200000
Normalised CTE | 0.98936 | 0.98936 | 1 | 1

## Slide 40: Validation case study
Material:
Plain weave, CF0504, (3K HTA 5131 carbon fibres, 200 gsm, 5 ends per cm)
10-ply laminates, created by resin film stacking :
(1) un-sheared (Vf =47.5%), (2) sheared at 16 degrees & (3) 20 degrees
Yarn width | Yarn height | Yarn in-plane spacing | Laminate thickness
1.76mm | 0.16mm | 2.03mm | 2.4mm
Fibre properties
E11 =235GPa, E22 = E33 =15GPa, v12 =0.3, v23 =0.3, G12=15, aL = -0.4x10-6/K,
aT = 10x10-6/K
Consolidation:
Autoclave at pressure of 6 bar
5 hours initial cure at 80°C
Ramp rate 2°C/min
After cooling below 60°C and release of pressure, free standing post-cure for 1 hour at 120°C
Hobbiebrunken, T., M. Hojo, K.K. Jin, and S.K. Ha, Influence of non-uniform fiber arrangement on microscopic stress and failure initiation in thermally and transversely loaded CF/epoxy laminated composites. Composites Science and Technology, 2008. 68(15–16): p. 3107-3113.
Fiedler, B., M. Hojo, S. Ochiai, K. Schulte, and M. Ochi, Finite-element modeling of initial matrix failure in CFRP under static transverse tensile load. Composites Science and Technology, 2001. 61(1): p. 95-105.
Pradere, C. and C. Sauder, Transverse and longitudinal coefficient of thermal expansion of carbon fibers at high temperatures (300–2500&#xa0;K). Carbon, 2008. 46(14): p. 1874-1884.
Matrix properties
E=2.7GPa
v=0.4
a = 40x10-6 /K after the full thermal cycle
Matrix:
MTM46 from CYTEC (previously ACG or UMECO

## Slide 41: Thermal expansion measurement
Warp
Weft
Sample cut angle θ
Samples
Table of sample cut angle θ (degree)
CTE measurement from dilatometer from samples orientated at various angles
Table of CTEs (x10-6/K)
Shear 0o |  | Shear 16o |  | Shear 20o | 
θ | CTE | θ | CTE | θ | CTE
0 | 2.12 | 0 | 2.36 | 0 | 2.99
45 | 2.32 | 37 | -6.23 | 15 | 0.25
90 | 2.02 | 74 | 3.93 | 30 | -3.3
 |  | 127 | 23.1 | 45 | -3.23
 |  |  |  | 60 | -0.97
 |  |  |  | 75 | 3.82
 |  |  |  | 90 | 8.46
 |  |  |  | 105 | 14.35
 |  |  |  | 120 | 18.49
 |  |  |  | 135 | 15.66
 |  |  |  | 150 | 13.1
 |  |  |  | 165 | 5.76
Shear 0o | Shear 16o | Shear 20o
0 | 0 | 0
45 | 37 | 15
90 | 74 | 30
 | 127 | 45
 |  | 60
 |  | 75
 |  | 90
 |  | 105
 |  | 120
 |  | 135
 |  | 150
 |  | 165
Chart: Angle to X-Axis (degrees)
| 0 | 45 | 90
No shear | 2.12 | 2.32 | 2.02
shear 16 degree | 2.36 | -6.23 | 3.93 | 23.1
shear 20 degrees | 5.76 | 13.1 | 15.66 | 18.49 | 14.35 | 8.46 | 3.82 | -0.97 | -3.23 | -3.3 | 0.25 | 2.99

## Slide 42
Model | CTE prediction in warp (x10-6/K) | 
Experiment | 2.12 | 
Infinite size in in-plane and thickness, zero nesting, represented by single layer with periodic boundary conditions | 3.20 | 
Ten layers, no nesting, pbc in-plane | 2.51 | 
Ten layers, random nesting, pbc in-plane (3 laminate models) | 2.17±0.01 | 
Weft
Warp
FE predictions- Shear 0o

## Slide 43
Converged mesh using 2 million elements - 100x100x200 (X Y Z)
HPC: 32CPUs, 69GB RAM, 130 minutes
FE Predictions – Shear 0°,16°& 20°
1

## Slide 44
Conclusions
Basic principles and assumptions have been used to refine fabric geometry to simulate realistic shear deformation.
The refinement process has been automated in TexGen and used to generate sheared unit cell models . These features are included in the latest TexGen release, version 3.6.0, www.texgen.sourceforge.net
CTE predictions based on FE thermo mechanical analysis showed good correlation with experimental results.
Laminate thickness and nesting were found to be significant geometric factors prediction of CTE in textile laminates.
Future work
Automation of laminate nesting in TexGen.
To predict manufacturing induced shape distortion by coupling unit cell and composite structural models.

## Slide 45
Acknowledgement
This work was supported by the Engineering and Physical Sciences Research Council [grant number: EP/IO33513/1], through the EPSRC Centre for Innovative Manufacturing in Composites.

## Slide 46: Braiding

## Slide 47: Braiding Facility
Robotic control of braider and robot
    Steeger 48 carrier braider and Kuka KR60 robot
    Synchronisation of braider speed to mandrel take-up speed
    Facility to braid large complex mandrel geometry
    Support structure to aid in braiding low density/brittle core materials (3D printed mandrels)
    Braid direction reversal: enables multi-pass braiding with minimal touch labour
    High axial tow deposition: Up to 96 tows per pass
    Load cells at the robot flange to measure force exerted by the braider
High deposition rate: Up to 1 metre of braid per minute
1D-Braid
In-house 3D printer to 3D print mandrels

## Slide 48: TexGen - Braiding
Added functionality to automatically build biaxial braided unit cells based on geometrical features such as tow size, shape and spacing.
Similar to work completed on woven fabrics, the braid module will enable material characterisation and permeability studies.
Developed as part of the TexGen code, shares common functionality with CTextile and integrated with CYarn for modelling.

## Slide 49: TexGen-Braiding
Allows for inputs of braider parameters such as speed and mandrel dimensions to calculate corresponding RUC.
Assign all yarns with the same properties or specify specific properties for each yarn.
Builds a geometrical based model of the RUC, this can be processed further through integration with Abaqus for mechanical properties or permeability calculations.

## Slide 50: Optimisation

## Slide 51: Novel manufacturing techniques for optimised fibre architectures
Optimisation framework:
With manufacturing constraints – manufacturable now e.g. vary yarn thickness/spacing and pattern in 3D weave
With relaxed manufacturing constraints – extend the search to cases non-constrained by current technologies
Novel preforming techniques:
Employ novel manufacturing techniques to implement new fibre architectures
Multi-axial preforms
Complex through-thickness reinforcement strategy
Preform with off-axis yarns
3D cylindrical preform with through-thickness binder
How to select a reinforcement which is most appropriate for a particular application? Can the optimal reinforcement be manufactured at the moment?
Project aims to develop a computational optimisation framework which can be used to drive design of fibre reinforcements

## Slide 52: Project Overview
Design-driven preforming
Identification of load cases
Structure
Part
Loading cases
Chart: Buckling coefficient
| 1.7279800000000001 | 1.3344100000000001 | 1.3344100000000001 | 1.7279800000000001 | 1.4615499999999999 | 1.51448 | 1.40357 | 1.51448 | 1.5679000000000001 | 1.5679000000000001 | 1.6186400000000001 | 1.6186400000000001 | 1.3764099999999999 | 1.4615499999999999 | 1.6638299999999999 | 1.6638299999999999 | 1.33691 | 1.7002299999999999 | 1.40357 | 1.7002299999999999 | 1.3764099999999999 | 1.7236100000000001 | 1.7236100000000001 | 1.33691 | 1.51448 | 1.51448 | 1.5679000000000001 | 1.5679000000000001 | 1.5679000000000001 | 1.51448 | 1.6638299999999999 | 1.51448 | 1.6638299999999999 | 1.51448 | 1.5679000000000001 | 1.6638299999999999 | 1.4615499999999999 | 1.51448 | 1.5679000000000001 | 1.6638299999999999 | 1.6638299999999999 | 1.5679000000000001 | 1.7002299999999999 | 1.5679000000000001 | 1.6186400000000001 | 1.51448 | 1.7002299999999999 | 1.7002299999999999 | 1.6638299999999999 | 1.6638299999999999
 | 21.7589 | 43.0017 | 43.0017 | 21.7589 | 36.2817 | 33.2108 | 37.8728 | 33.2108 | 30.4874 | 30.4874 | 28.1323 | 28.1323 | 40.457 | 36.2817 | 26.1193 | 26.1193 | 41.6824 | 24.4125 | 37.8728 | 24.4125 | 40.457 | 22.9738 | 22.9738 | 41.6824 | 33.2108 | 33.2108 | 30.4874 | 30.4874 | 30.4874 | 33.2108 | 26.1193 | 33.2108 | 26.1193 | 33.2108 | 30.4874 | 26.1193 | 36.2817 | 33.2108 | 30.4874 | 26.1193 | 26.1193 | 30.4874 | 24.4125 | 30.4874 | 28.1323 | 33.2108 | 24.4125 | 24.4125 | 26.1193 | 26.1193
Optimisation of preform
Unit cell model
Optimisation
Properties evaluation
New preforming technologies will consider both optimal reinforcement and component geometry
Optimal solution for a part
Development of a process to enable manufacture

## Slide 53: Optimisation framework
Evaluation of objective function
(macro-scale simulations)
Initial design of preform
Homogenisation
(meso-scale simulation)
Improved design
Part geometry
A
B
B
D
( )
Problem
Optimisation framework
New model based on GA “recommendations”
Aim: maximise bending stiffness with no increase of weight
Bending stiffness
Stiffness matrix
Optimisation
Genetic algorithm:
Compares evaluated designs
Evolves good designs (mutation)
Takes best features of good results (cross-over)
Relaxed manufacturing constraints
Parametrised geometry of meso-scale model
New geometry parameters

## Slide 54: T-Piece Modelling

## Slide 55: Weave Variations
Variation I
Variation II
Warp & Binder
Weft
Resin-rich noodle region

## Slide 56: Weave Patterns
Double weft insertion
Web
Flange, Variation I
Flange, Variation II

## Slide 57: Input File Format
Warp stack
Binder yarn
Python script reads input file and creates textile using TexGen COrthogonalTextile class
Build cell array, specifying warp/weft/binder yarn locations

## Slide 58: As-woven T-Piece Models
Extra information saved from weave pattern ensures:
Correct representation of weft yarns crossing from one warp stack to another
Correct paths for weft yarns changing vertical position with the cell array
Variation I
Variation II
Crossover weft yarn
Crossover where vertical position in weft yarns changes not captured in variation II

## Slide 59: Transformed T-Pieces
Bending of warp yarns and rotational and translational transformations and are applied to the as-woven models using a Python script.
Variation I
Variation II

## Slide 60: Modelling Deformation in Knitted Fabrics

## Slide 61: Knitted Textile for use as Fabric Sensor
Material measurements used to create parameterised model
Parameter | Measurement /µm
Radius, r | 216
Height, ly | 363
Height, sy | 1107
Width, sx | 406

## Slide 62: Initial Idealised Model
Model created using actual textile measurements with constant, circular cross-sections
Intersections

## Slide 63: Modification of Cross-Sections
Hybrid cross-sections defined and assigned to specific nodes

## Slide 64: Deformation Simulation
TexGen dry fibre export generates conformal mesh and .inp for ABAQUS/Explicit simulation
Used ABAQUS General Contact algorithm
Unit cell with periodic boundary conditions
3x3 unit cell, unconstrained in x direction

## Slide 65: TexGen Modelling Theory

## Slide 66
Generating a Textile
Each step individually using either GUI, Python script or C++ API functions
Steps combined and performed automatically in 2D and 3D wizards
3 - Specify domain
4 - Output data
  Create yarn path
  Assign sections
  Select interpolation
  Assign repeats
  Assign fibre properties
1 - Create Textile
2 - Add yarns

## Slide 67: Yarn Specification
Yarns are denotes by a set of Master Nodes
A path is generated between the master nodes by an interpolation function
Periodic to maintain continuity across yarn repeats
  Bezier spline
  Natural cubic spline
  Linear spline

## Slide 68: Yarn Cross-Sections - Interpolation
Yarn cross-sections are specified as 2D sections perpendicular to the yarn tangent
By default the cross-section is constant along the length of the yarn or an interpolation method can be chosen
GUI: Select Modeller -> Assign Section
  Select interpolation
    Constant
    Interpolate between nodes
    Interpolate between positions

## Slide 69: Yarn Cross-Sections – Section Specification
Cross-sections are specified at the locations given by the section interpolation
Available cross-sections:
  Ellipse
  Lenticular
  Power ellipse
  Hybrid
  Rectangle
    Use rather than power ellipse with power = 0 to generate uniform section meshes
  Polygon
    Only by scripting

## Slide 70: Power Ellipse Cross-Section
=
=
Specialisation of the Superellipse discovered by Gabriel Lame*
*M. Gardner, editor.Mathmatical Carnival. Vintage, 1977

## Slide 71: Building Yarns
Generates yarn path using specified interpolation function
  Creates a set of slave nodes along the interpolated path at the specified resolution
Generates cross-sections for each slave node, interpolating between specified cross-sections where necessary
Generates surface by joining points on adjacent cross-section
Yarn.SetResolution function assigns number of section points and, optionally, number of slave nodes
SetResolution(20)
SetResolution(40)
SetResolution(40,20)

## Slide 72: Yarn Repeats and Domain
Yarn repeats allow a given yarn section to be repeated as specified by a set of vectors (in theory, allowing an infinite textile)
The domain restricts the model to a specific region
  Specified by a set of convex planes
  Typically, but not always, the unit cell

## Slide 73: TexGen File Format
tg3 file – basically a renamed xml file
  Three versions containing different levels of data
    Minimal – textile data only (generated by the weave classes)
    Standard – textile and yarn data
    Full – textile, yarn and mesh data
Notes: Slave nodes generated along yarn path, number depending on resolution, then used to create mesh

## Slide 74: Automatic Generation of 2D Weaves

## Slide 75: Automatically Generated Textiles
Predefined weave patterns are generated using classes which use Ctextile as a base class. They are used to input weave pattern information which then automatically generate the yarns.

## Slide 76: CTextileWeave2D
The 2D wizard in the TexGen GUI creates weaves using the CTextileWeave2D class
0 , 0
1 , 0
1 , 1
Warp 0
Warp 1
Weft 0
Weft 1
0 , 1
Whether the warp and weft are up or down is stored for each x,y position
x, y position
Values stored: 0, 1
(Weft down, warp up)

## Slide 77: CTextileWeave2D
The 2D wizard in the TexGen GUI creates weaves using the CTextileWeave2D class
0 , 0
1 , 0
1 , 1
Warp 0
Warp 1
Weft 0
Weft 1
0 , 1
Whether the warp and weft are up or down is stored for each x,y position
x, y position
Values stored: 0, 1
(Weft down, warp up)
GUI: Set using Weave Pattern dialog
Python:
weave = CTextileWeave2D( numWefts,… numWarps,spacing, thickness )
weave.SwapPosition(0, 0)
weave.SwapPosition(1, 1)

## Slide 78: Saving TexGen models

## Slide 79: Save File Format
tg3 file – basically a renamed xml file
  Three versions containing different levels of data
    Minimal – textile data only (generated by the weave classes)
    Standard – textile and yarn data
    Full – textile, yarn and mesh data
Notes: Slave nodes generated along yarn path, number depending on resolution, then used to create mesh

## Slide 80: Saving Images
Outputting images
File -> Save Screenshot
Saves as .png file
Increase magnification to export with higher resolution
Use Render->Change Background Colour to change to white (or desired) background

## Slide 81: Exercise – Create 2D Weave
 | Yarn width / mm | Yarn height / mm | Yarns / cm
Warp | 0.9 | 0.3 | 10
Weft | 0.7 | 0.2 | 13
Create a 4x4 satin weave textile using the 2D weave wizard using the parameters in the table

## Slide 82: Layered and Rotated Textiles

## Slide 83: Layered Textiles
LayeredTextile = CTextileLayered()
# Add the first layer with specified offset
Offset = XYZ(0.25, 0.5, 0)
LayeredTextile.AddLayer( weave, Offset );
# Add the second textile to the layered textile
LayeredTextile.AddLayer( weave1, Offset )
Create layered textiles for simulation of laminates
Textiles->Create Layered option in the GUI
  Select textiles and order of stacking, including rotated textiles
Or Select number of layers from 2D wizard
Domain defaults to size of largest weave pattern
Using the Python scripting API:

## Slide 84: Layer Offsets
Textiles created with user interface are generated without offsets
Apply offsets either in GUI or Python scripting
Constant offset applied between each pair of layers
Random offset generated for each layer
Manually select offsets for each layer
Constant x offset
Random offsets

## Slide 85: Nesting
Two options for automatic nesting
Retain pre-set offsets
Maximum nesting – find offset between each pair of layers which will allow the minimum distance between layers without intersections
Random offsets, t = 0.65mm
Nested, retained offsets
t = 0.57mm
Nested, maximum nesting
t = 0.506mm

## Slide 86: Rotate Textile
Textiles -> Rotate Textile
Choose rotation axis
Select whether to rotate domain
Original domain
Rotated domain
Layered textile including rotated layers

## Slide 87: Automatic Generation of 3D Weaves

## Slide 88: Automatically Generated 3D Weaves
These all use the CTextile3DWeave base class
Creates a grid of points at the yarn crossovers, specified in the GUI by the Weave Pattern dialog
Each point may be warp, weft or no yarn
The derived classes then automatically generate the yarn paths from this data
Textiles using the base class can be created using a Python script
1
5
3
7
0
k
10
9
0
1
2
3
j
1
2
i
Cell(1,0)

## Slide 89: Exercise – Create 3D Orthogonal Weave
 | Yarn width /mm | Yarn height /mm | Yarn spacing /mm | Yarn fibre diameter /mm | Fibres per yarn
Warp | 3.6 | 0.35 | 3.8 | 0.007 | 5000
Weft | 2.58 | 0.25 | 2.8 | 0.007 | 8000
Binder | 1.375 | 0.16 | 1.4 | 0.007 | 3500
Create a 3D orthogonal weave textile with 6 warp yarns (2 warp stacks to 1 binder yarn) and 4 weft yarn stacks.
3 yarns/weft stack, 2 yarns/warp stack
Textile thickness = 1.4mm
Use the table for remaining parameters

## Slide 90: Manually creating textiles

## Slide 91: Export

## Slide 92: Yarn Properties
To export element volume fractions set up yarn properties, either for whole textile (all yarns same) or individual yarns
Modeller -> Assign Yarn Properties
Requires
Total fibre area
Or
Fibre density and yarn linear density
Or
Fibre diameter and number of fibres per yarn
Mechanical properties
Select required yarns then Modeller -> Assign Yarn Properties
to set Young’s modulus, Shear modulus, Poisson’s ratio and coefficient of thermal expansion
Select Modeller -> Assign Matrix Properties to set matrix properties

## Slide 93: ABAQUS Voxel Export
GUI: Select File -> Export -> ABAQUS File -> ABAQUS Voxel File
Hex elements
Periodic boundary conditions and steps for extraction of material properties
http://texgen.sourceforge.net/index.php/Extraction_of_Material_Properties_using_Voxel_Meshing_and_Abaqus
All ABAQUS exports include additional .ori and .eld files containing element orientation, fibre volume fraction and yarn information.

## Slide 94: ABAQUS Dry Fibre Export
GUI: Select File -> Export -> ABAQUS File -> ABAQUS Dry FibreFile
Conformal mesh using hex and wedge elements
Uses weave pattern information to generate contact surfaces
Correction for small intersections

## Slide 95: Conformal Mesh
Volume Mesh
GUI: Select File -> Export -> Volume Mesh
Tetrahedral elements
Save as ABAQUS .inp file or .vtu
Works best for 2D weaves
Tetgen Export
GUI: Select File -> Export -> Tetgen Mesh
Tetrahedral elements
Save as ABAQUS .inp file
May need to introduce gap between yarns for export to be successful
Uses Tetgen library: http://wias-berlin.de/software/index.jsp?id=TetGen&lang=1

## Slide 96: Geometry Export
The geometry alone can be exported in IGES, STEP or stl format. No orientations, volume fractions or properties are exported.
GUI: Select File -> Export -> IGES File
or -> STEP File
This option uses the OpenCASCADE library.
The ‘Smooth’ option may be unsuccessful for more complex geometries
‘Join Yarn Sections’ will remove joins at repeat boundaries but is much slower
GUI: Select File -> Export -> Surface Mesh
Exports the surface mesh as displayed by Rendering -> X-Ray
Saves in .vtu or .stl format

## Slide 97: Geometry Export
IGES and STEP export
Uses OpenCASCADE package to generate these
Exports only the geometry
Lose any orientation and volume fraction information
Surface Mesh exportExports the surface mesh as shown by the Rendering -> X-Ray option
Surface mesh as shown by the Rendering -> X-Ray option
Export with or without the domain
VTK unstructured grid file (.vtu)
ASCII or binary STL file (.stl or .stlb)
SCIRun file (.pts)
.vtu surface mesh displayed in Paraview

## Slide 98: TexGen as a Pre-processor for Generating Textile Models

## Slide 99: Workflow for finite element elastic analysis
TexGen geometry model (.TG3) file
TexGen export of Abaqus input (.INP) file
Customisation of .INP file
Abaqus simulations
* Elastic * Thermo-mechanical * (Damage)
Abaqus script for result file (.ODB) exploitation. RVE material properties
Material properties for yarn fibres and matrix (manufacturer data)
Micro-scale simulation for yarn material properties
Reporting of results:
* Material properties
* Stress fields * Strain fields

## Slide 100: Material continuum assumption
  Displacement field under overall macroscopic strains:
    3 direct strains
    3 shear strains
  “Correct” BC approach: equivalent continuum, tie to 6 “driver points”
  Recover relationship between stresses and strains (elastic props)

## Slide 101: Periodic BCs: 3D and “untied”
  “Correct” BC approach of Li and Wongsto
  Full 3D boundary conditions: infinitely repeating 3D continuum
  Not true for tests!

## Slide 102: Periodic BCs: 3D and “untied”
  Also tried “untying” the through-thickness constraints
  Represents repeating units only in-plane, free surfaces top and bottom
  Differences in results actually insignificant

## Slide 103: Evaluation of yarn component properties
Fibre properties (HTS40 F13)
Input yarn material properties: 7micron fibre at 76% vol. UD hexagonal packing
E1 | E2 | E3 | v13 | v12 | v32 | G12 | G23 | G31
183.1 | 9.67 | 9.67 | 0.23 | 0.23 | 0.43 | 5.66 | 3.37 | 5.66
 | Ex | ν
Fibre | 238.6 | 0.20
Resin | 3.1 | 0.35

## Slide 104: FE prediction
Mesh size | E1 | E2 | v12 | v21 | G12
40-50-30 | 34 | 64 | 0.03 | 0.05 | 3.06
Step 1: export ABAQUS .inp file
Step 2: lauch ABAQUS Solver with command line:
ABAQUS job=Filename
Step 3: extract material properties from .odb file:
Use the dataHandling.py and effectiveMatPropRVE.py files supplied with TexGen to calculate the material properties http://texgen.sourceforge.net/index.php/Extraction_of_Material_Properties_using_Voxel_Meshing_and_Abaqus

## Slide 106
Exporting volume mesh from TexGen
Open a TexGen model ready in TexGen window. Click “File -> Export -> Volume Mesh…”, a dialog window appears as below. Once the parameters are set and click ok, a volume mesh file is created, either in .vtk or .inp format.
1.a This controls the number of element nodes. Linear results in 4 noded tetrahedrons while Quadratic results in 10 noded tetrahedrons.
1.b Option for Quadratic meshing only.
1.c Create the matching meshes on opposite faces to ensure periodic interface.
1.f Any gap between yarns smaller than this tolerance will be merged to avoid bad quality elements.
1.e Controls the mesh density and it approximates the edge length of elements.
1.d Sets up periodic boundary conditions. Select None.

## Slide 107
2. Importing volume mesh to CFX
Launch ANSYS CFX -> CFX Pre 13.0. Go to File and then New Case, choose General as Simulation Type and click OK. Go to File -> Import -> Mesh, an Import Mesh window comes up. After the steps 2.a-d, click Open. The mesh is now imported.
2.a Go to the folder where the volume mesh .vtu file is allocated
2.b Choose User Import (*) as in Files of type
2.c Choose mm as mesh unit
2.d If importing .vtk file choose CFXImportVTK.exe which is available on Sourceforge.

## Slide 108
3. Editing mesh in CFX
To organise the domain surfaces mesh into 6 separate regions which will be used for defining boundary conditions.
3.a Select the domain region to edit
3.b Click Start Picking
3.e Name the selected face and click Apply. Repeat 3.a to 3.e till all 6 faces are separate.
3.c Choose Flood Select
3.d Click on the face to be moved

## Slide 109
4. Defining domains in CFX
To define the fluid domain for the gaps between yarns only.
New domains are created by selecting Insert > Domain or clicking the Domains icon. Note that creation of domains from the menu bar or toolbar may subsequently require selection of the appropriate analysis type. Domains can also be created by right-clicking the appropriate analysis type in the Outline view.
For the fluid domain, the default setting is recommend in the Basic Settings Tab, and in Fluid Models Tab a None (Laminar) option is chosen for Turbulence Model.
Click OK/Apply

## Slide 110
5. Domain interface
2 sets of interfaces is to be defined. 2 sets of fluid fluid interface with translational periodicity at opposite faces of the domain;
3.a Click Domain Interface icon.
3.b Select Interface Type: fluid-porous, fluid fluid or porous porous
3.c Select corresponding domain and surfaces on both sides of interface. Click to get complete lists.
3.d Interface Model: General Connection is used at fluid porous yarn interface while Translational Periodicity is for opposite faces

## Slide 111
6. Boundary conditions
To define pressure drop on two faces along Z direction. Click Boundary icon
In Basic Settings Tab, Boundary Type is chosen as Opening. Since the boundary surface is very close to fabric, Opening option allows the fluid to cross the boundary surface in either direction. Choose the appropriate region for Location.
In Boundary Details Tab, set the relative pressure in Pa.
7. Initialisation
Click the global initialisation icon to assign all the unspecified solution field values (an Initial Guess).

## Slide 112
8. Solver Control
Right click Solver Control in Outline, select Edit.
In Basic Settings Tab, Convergence control, set the maximum iteration to 1000. Convergence Criteria: Set Residual Type as RMS, Residual Target to 1E-5.
9. Run Solver and Monitor
To start the analysis by clicking
The simulation will terminate once the convergence criteria is satisfied or it reaches the maximum iterations.

## Slide 113
10. CFD results
In CFX-Solver Monitor Window, when the simulation terminates normally, check Post-Process Results and click OK or launch CFD-Post by click Icon
How to calculate fabric permeability?
Go to Calculator Tab, choose Function Calculator. To obtain the values of flow cross-section area (A), areaAve pressure at the inlet (P1) and at the outlet (P2), mass flow rate at either inlet or outlet (m’). Given the air at 25c, its density (ρ) is 1.185kg/m3, and its dynamic viscosity (μ) is 1.831E-5 Pa s. L is the unit cell thickness. Fabric permeability (k) follows Darcy’s law

## Slide 114: Python Scripting

## Slide 115: Documentation
User Guide for the TexGen GUI:
  http://texgen.sourceforge.net/index.php/User_Guide
API Reference Guide:
  http://texgen.sourceforge.net/api/
Scripting Guide with sample scripts:
  https://github.com/louisepb/TexGenScriptingGuide

## Slide 116
Generating a Textile
Each step individually using either GUI, Python script or C++ API functions
Steps combined and performed automatically in 2D and 3D wizards
3 - Specify domain
4 - Output data
  Create yarn path
  Assign sections
  Select interpolation
  Assign repeats
  Assign fibre properties
1 - Create Textile
2 - Add yarns

## Slide 117: Create Textile
Each textile is created in a Ctextile object
Textile = CTextile()
GUI: Select Textiles -> Create Empty ( Step 1 )
Python:

## Slide 118: Create Yarns
Yarn = CYarn()
Yarn.AddNode(CNode(XYZ(0,0,0)))
Yarn.AddNode(CNode(XYZ(5,0,1)))
Yarn.AddNode(CNode(XYZ(10,0,0)))
Yarns are denotes by a set of Master Nodes
GUI: Select Modeller->Create Yarn ( Step 2 )
Python:

## Slide 119: Interpolation Between Nodes
Yarn.AssignInterpolation(CInterpolationCubic())
GUI: Select Modeller -> Interpolation
  Bezier spline
  Natural cubic spline
  Linear spline
  Periodic – select to maintain continuity across yarn repeats
A path is generated between the master nodes by an interpolation function
Python:
Defaults to periodic, send False as parameter to CInterpolationCubic() for non-periodic interpolation

## Slide 120: Yarn Repeats
Yarn repeats allow a given yarn section to be repeated as specified by a set of vectors (in theory, allowing an infinite textile)
GUI: Select Modeller -> Assign Repeats
  Specify a set of repeat vectors
Python:
Yarn.AddRepeat(XYZ(10,0,0))
Yarn.AddRepeat(XYZ(5,5,0))
Textile.AddYarn(Yarn)

## Slide 121: Domain
The domain restricts the model to a specific region
  Specified by a set of convex planes
  Typically, but not always, the unit cell
GUI:
Select Domain -> Create Box
  Input minimum and maximum x,y,z values for bounding box
Or
Select Domain -> Create Planes
  Input required number of planes specified by the unit normal to the plane and its distance from the origin
Python:
Textile.AssignDomain(CDomainPlanes(XYZ(-5,-2,-1),XYZ(15,12,2)))
AddTextile(“Workshop”, Textile)
Planes = PlaneVector
Planes.push_back(PLANE( XYZ(1,0,0), 0)) #Repeat for set of planes
Textile.AssignDomain(CDomainPlanes( Planes ))
AddTextile(“Workshop”, Textile)
or:

## Slide 122: Assigning Sections to a Yarn
Cross-sections are created and assigned to an object derived from the CYarnSection and CYarnSectionInterp base classes which is then assigned to a yarn
Classes correspond to the 3 options in the Select Yarn Section dialog
YarnSections = CYarnSectionInterpNode()
YarnSections.AddSection( CSectionLenticular(1.0,0.5,0.1) )
YarnSections.AddSection( CSectionPowerEllipse(1.0,0.5,0.4,0.25) )
Yarn.AssignSection( YarnSections )
Python:
YarnSections = CYarnSectionConstant( CSectionEllipse(1.0,0.5) )
Yarn.AssignSection( YarnSections )
YarnSections = CYarnSectionInterpPosition()
YarnSections.AddSection( 0.0, CSectionLenticular(1.0,0.5,0.1) )
YarnSections.AddSection( 0.5, CSectionEllipse(1.0,0.5) )
Yarn.AssignSection( YarnSections )

## Slide 123: Creating Sections
Shape = CSectionEllipse( width, height)
Shape = CSectionLenticular( width, height, distortion)
Shape = CSectionPowerEllipse( width, height, power, xoffset)
Shape = CSectionRectangle( width, height)
Shape = CSectionEllipse( width, height)
Syntax for creating different shaped sections:

## Slide 124: Polygon Sections
Points = XYVector()
Points.push_back(XY(1.47887, -0.080294))
Points.push_back(XY( 1.1267, 0.0421169))
:
:
Points.push_back(XY( 1.10991, -0.133933))
Shape = CSectionPolygon(Points)
Set up a vector of xy points and then use this to create the polygon section:

## Slide 125: Hybrid Sections
Hybrid sections are generated by combining several different sections
GUI: Select Hybrid in the Select Cross-section Shape dialog
Click on 2 or more points outside the shape in the lower window to specify the divisions for the shapes to be assigned.
Click within each section in turn to specify the shape to be used.

## Slide 126: Hybrid Sections
# Specify two sections with a horizontal division
Top = CSectionEllipse( 1.0, 0.4 )
Bottom = CSectionPowerEllipse( 1.0, 0.4, 0.4, 0.25 )
Hybrid = CSectionHybrid( Top, Bottom )
Python:
# Specify four sections in quadrants
Hybrid = CSectionHybrid( TopRight, TopLeft, …
BottomLeft, BottomRight )
# Specify individual parts
HybridSection = CSectionHybrid()
# Add as many divisions as required
Hybrid.AddDivision(0)
Hybrid.AddDivision(0.3)
# Specify section for each division
Hybrid.AssignSection(0, CSectionLenticular(1.0,0.4))
Hybrid.AssignSection(1, CSectionEllipse(1.0,0.4))

## Slide 127: Rotated Sections
Sections can be rotated. Create the required section and then rotate
CSectionRotated(CSectionEllipse(1, 0.1), math.radians(45))
Python:

## Slide 128: Yarn Cross-Sections – Python Implementation
YarnSections = CYarnSectionInterpNode()
YarnSections.AddSection( CSectionLenticular(1.0,0.5,0.1) )
YarnSections.AddSection( CSectionPowerEllipse(1.0,0.5,0.4,0.25) )
# Hybrid Section
Top = CSectionEllipse( 1.0, 0.4 )
Bottom = CSectionPowerEllipse( 1.0, 0.4, 0.4, 0.25 )
YarnSections.AddSection( CSectionHybrid( Top, Bottom ) )
Yarn.AssignSection( YarnSections )
Python:

## Slide 129: Model with Multiple Yarns
Create a list of yarns
Add nodes to each yarn
# Create a Python list containing 4 yarns
Yarns = [CYarn(), CYarn(), CYarn(), CYarn()]
# Add nodes to the yarns to describe their paths
Yarns[0].AddNode(CNode(XYZ(0, 0, 0)))
Yarns[0].AddNode(CNode(XYZ(0.22, 0, 0.05)))
Yarns[0].AddNode(CNode(XYZ(0.44, 0, 0)))
Yarns[1].AddNode(CNode(XYZ(0, 0.22, 0.05)))
Yarns[1].AddNode(CNode(XYZ(0.22, 0.22, 0)))
Yarns[1].AddNode(CNode(XYZ(0.44, 0.22, 0.05)))
…
Python:

## Slide 130: Populate Yarn Data
Use a for loop to iterate through yarns
Assign sections, resolution, repeats for each yarn
Add the yarn to the textile
for Yarn in Yarns:
# Set the interpolation function
Yarn.AssignInterpolation(CInterpolationCubic())
# Assign a constant cross-section of elliptical shape
Yarn.AssignSection(CYarnSectionConstant(CSectionEllipse(0.18, 0.04)))
# Set the resolution of the mesh created
Yarn.SetResolution(20)
# Add repeat vectors to the yarn
Yarn.AddRepeat(XYZ(0.44, 0, 0))
Yarn.AddRepeat(XYZ(0, 0.44, 0))
# Add the yarn to our textile
Textile.AddYarn(Yarn)
Python:

## Slide 131: Exercise – Edit Polyester.py
Change the cross-sections to lenticular.
Change the cross-section dimensions: Width = 0.2, height = 0,048
Change the height of the domain to suit the amended yarn dimensions so that it does not cut off any of the yarns.
Change the yarn resolution to 40

## Slide 132: Using Weave Classes in Scripts
Use the constructor for the appropriate weave type
Use the SwapPostion functions to set up the weave pattern
Look at the API reference to find functions for specific types
Textile = CTextileWeave2D(4, 4, 5, 2, False);
# Set the weave pattern
Textile.SwapPosition(3, 0);
Textile.SwapPosition(2, 1);
Textile.SwapPosition(1, 2);
Textile.SwapPosition(0, 3);
# Adjust the yarn width and height
Textile.SetYarnWidths(4);
Textile.SetYarnHeights(0.8);
# Setup a domain
Textile.AssignDefaultDomain()
AddTextile(Textile)
Python:

## Slide 133: Assigning Yarn Colour
RenderWin = GetRenderWindow()
# Change x yarns to grey
for x in range (0, 4):
RenderWin.SetYarnColor(x, COLOR(0.5, 0.5, 0.5))
# Change y yarns to purple
for y in range (4, 8):
RenderWin.SetYarnColor(y, COLOR(0.5,0,0.5))
Colour change will remain until yarn is selected

## Slide 134: Resources
User Guide: http://texgen.sourceforge.net/index.php/User_Guide
Scripting Guide:
https://github.com/louisepb/TexGenScriptingGuide
TexGen source code:
https://github.com/louisepb/TexGen
Workshop materials:
https://github.com/louisepb/ICMAC2018-Workshop